Satisfying the requirement for Safety Glass in critical locations

1 Glazing in doors

Glazing in doors which is wholly or partially within 1500mm from floor level shall be: Minimum Class C to BS 6206:1981 and marked according to BS 6206.

2 Glazing adjacent to doors

Glazing which is wholly or partially within 300mm of the edge of a door and wholly or partially within 1500mm of floor level shall be: Minimum

Class C to BS 6206 and marked to BS 6206. Note: In both 1& 2, if the smaller dimension of the pane is greater than 900mm it shall be:

Minimum Class B to BS 6206 and marked according to BS 6206.

3 Low level glazing (excluding guarding)

not covered by 1 or 2

Glazing which is wholly or partially within 800mm of the floor level shall be: Minimum Class C to BS 6206 and marked according to BS 6206.

Exceptions

• Panes having the smaller dimension less than 250mm and of area less than 0.5m2 may be minimum 6mm (nominal) thick glass not complying with BS 6206

• Panes forming parts of fronts (but not other locations) to shops, showrooms, offices, factories and public buildings, supported on all

edges, may be of equivalent robustness not complying with BS 6206:

8mm must not exceed 1100 x 1100mm

10mm must not exceed 2250 x 2250mm

12mm must not exceed 3000 x 4500mm

15mm (and thicker) – no limit

• Panes protected by a suitably designed barrier

4 Stairs, ramps and barriers

• England and Wales – ‘The Building Regulations 1991 Part K:

Stairs Ramps and Guards’ 300mm

Doors Glazing

Adjacent to doors Low level glazing Safety glass is not a requirement here

300mm

1500mm

800mm

For new buildings and for buildings subject to major refurbishment, the requirements for glazing when incorporated in the designs for stairs,

ramps and barriers can be found in the following documents: Approved document K “Protection from falling, collision and impact”

BS 6180:1999 and BS 6399: Part 1: 1996 “Code of practice for dead and imposed loads”.

5 Overhead glazing

In most types of buildings, in sloping or horizontal overhead glazing situations, it is generally regarded as appropriate to install

glass which will either tend to stay in place if it is cracked Laminated Safety Glass to fracture into relatively harmless pieces (Pilkington T glass)

which are less likely to cause serious injury, if they fall, than sharp shards of annealed glass. Further guidance can be found in BS 5516, briefly summarised in Table 1. There are some exceptions to these requirements

for safety glass, based on the robustness of annealed glass.